Prop treatment:

1.  Degrease using Interlux Fiberglass Solvent Wash #202 or Special Thinner #216

2.  Sand to bright metal using coarse emory cloth or sand blast.

3.  Remove all dust with a clean rag

4.  Wipe again with Fiberglass Solvent Wash #202 or Special Thinner #216

5.  Immediately after step 4, Apply ONE THIN coat of Interlux Vinyl-Lux

Primewash #353/354 thinned 25% with Vinyl-Lux Solvent #355

6.  Allow Vinyl-Lux Primewash to dry a MINIMUM of 1 hour but NO MORE than 24 hours and apply FOUR coats of Interprotect 2000E/2001E following the dry times

on the label.

7.  Apply 2 to 3 coats of hard bottom paint (Pettit Trinadad) following dry times on the label.

